DRS系列辐射交联

# 低温收缩阻燃型套管

# Flexible Heat Shrinkable Thin Wall Cross-linked Polyolefin Tubing

CHARACTERISTICS:

| Property | Test Condition | Performance |
| --- | --- | --- |
| Tensile strength |  | 12Mpa minimum. |
| Elongation |  | 400% minimum. |
| Tensile strength after aging | After 7 Days Air Oven at 158(C | 10Mpa minimum. |
| Elongation after aging |  | 300% minimum |
| DEFORMATION TEST | 1 hr at 131(C | 25% maximum. |
| HEAT SHOCK TEST | 4hr at 250(C | No Cracking |
| FLEXIBILITY TEST | 7 Days Air Oven at 158(C | No Cracking, No Permanent Deformation |
| CONDUCTOR CORROSION | 7 Days Air Oven at 158(C | No Corrosion |
| Volume Resistivity |  | 1014 (.cm minimum. |
| Dielectric withstand |  | No Breakdown for 60 sec.at 2.5KV |
| Breakdown voltage |  | 10KV minimum. |
| Dielectric Strength |  | 25 KV/mm minimum. |
| Dielectric withstand after aging | After 7 Days Air Oven at 158(C | No Breakdown for 60 sec.at 2.5KV |
| Breakdown voltage after aging |  | 10KV minimum |
| COLD BEND TEST | 1hr at -30(C | No Cracking |
| LONGITUDINAL CHANGE | 3 minute Air Oven at 200(C | ( 5% |
| ECCENTRICITY |  | 30% maximum. |
| Flammability |  | VW-1 |
| Minimum Complate Shrink Temperature |  | 90(C（3 minute） |

# DRS系列主要性能指标:

| 测试项目 | 测试条件 | 测试结果 |
| --- | --- | --- |
| 拉伸强度 |  | ( 12Mpa |
| 断裂伸长率 |  | ( 400% |
| 老化后拉伸强度 | 158(C 烘箱中 放置7天后 | ( 10Mpa |
| 老化后断裂伸长率 |  | ( 300% |
| 热变形试验 | 131(C ，1小时 | ( 25% |
| 热冲击试验 | 250(C，4小时 | 不破裂 |
| 弹性试验 | 158(C，烘箱中7天 | 不破裂、无永久形变 |
| 铜腐蚀试验 | 158(C，烘箱中7天 | 无腐蚀 |
| 体积电阻系数 |  | ( 1014 (.cm |
| 绝缘试验 |  | 2.5KV 60秒 不击穿 |
| 工频耐压强度 |  | ( 10 KV |
| 击穿强度 |  | ( 25KV/mm |
| 老化后绝缘试验 | 158(C 烘箱中 放置7天后 | 2.5KV 60秒 不击穿 |
| 老化后工频耐压强度 |  | ( 10 KV |
| 低温弯曲试验 | -30(C，1小时后 | 不破裂 |
| 纵向收缩比 | 200(C烘箱收缩3分钟 | ( 5% |
| 偏壁率 |  | ( 30% |
| 阻燃性能 |  | VW-1 |
| 完全收缩温度 |  | 90(C（3 分钟） |

DRS系列低温收缩阻燃型套管规格表 STANDARD SIZE：

| 规格 （mm） | 收缩前内径 （mm） | 收缩前壁厚 （mm） | 收缩后内径 （mm） | 收缩后壁厚 （mm） | 包装长度 （m/卷） |
| --- | --- | --- | --- | --- | --- |
| 1.0/0.5 | 1.4(0.3 | 0.2(0.05 | 0.4(0.1 | 0.40(0.05 | 200 |
| 1.5/0.75 | 1.9(0.3 | 0.2(0.05 | 0.6(0.1 | 0.40(0.05 | 200 |
| 2.0/1.0 | 2.4(0.3 | 0.25(0.05 | 0.9(0.1 | 0.45+0.1 | 200 |
| 2.5/1.25 | 2.9(0.3 | 0.25(0.05 | 1.1(0.1 | 0.45+0.1 | 200 |
| 3.0/1.5 | 3.4(0.3 | 0.25(0.05 | 1.4(0.1 | 0.45+0.1 | 100 |
| 3.5/1.75 | 3.9(0.3 | 0.25(0.05 | 1.6(0.1 | 0.45+0.1 | 100 |
| 4.0/2.0 | 4.4(0.3 | 0.25(0.05 | 1.8(0.1 | 0.45+0.1 | 200 |
| 4.5/2.0 | 4.9(0.3 | 0.35(0.05 | 1.9(0.1 | 0.60+0.1 | 100 |
| 5.0/2.5 | 5.4(0.3 | 0.35(0.05 | 2.3(0.2 | 0.55+0.1 | 100 |
| 6.0/3.0 | 6.4(0.4 | 0.35(0.05 | 2.8(0.2 | 0.55+0.1 | 100 |
| 7.0/3.5 | 7.4(0.4 | 0.35(0.05 | 3.3(0.2 | 0.55+0.1 | 100 |
| 8.0/4.0 | 8.4(0.4 | 0.35(0.05 | 3.8(0.2 | 0.55+0.1 | 100 |
| 9.0/4.5 | 9.4(0.4 | 0.35(0.05 | 4.3(0.2 | 0.55+0.1 | 100 |
| 10.0/5.0 | 10.5(0.4 | 0.35(0.05 | 4.8(0.2 | 0.60+0.1 | 100 |
| 11.0/5.5 | 11.5(0.4 | 0.35(0.05 | 5.3(0.2 | 0.60+0.1 | 100 |
| 12.0/6.0 | 12.5(0.4 | 0.35(0.1 | 5.7(0.3 | 0.70+0.1 | 100 |
| 13.0/6.5 | 13.5(0.4 | 0.35(0.1 | 6.2(0.3 | 0.70+0.1 | 100 |
| 14.0/7.0 | 14.5(0.4 | 0.35(0.1 | 6.7(0.3 | 0.70+0.1 | 100 |
| 15.0/7.5 | 15.5(0.5 | 0.35(0.1 | 7.2(0.3 | 0.70+0.1 | 100 |
| 16.0/8.0 | 16.5(0.5 | 0.35(0.1 | 7.7(0.3 | 0.70+0.1 | 100 |
| 17.0/8.5 | 17.5(0.5 | 0.35(0.1 | 8.2(0.3 | 0.70+0.1 | 100 |
| 18.0/9.0 | 19.0(0.5 | 0.4(0.1 | 8.7(0.3 | 0.80+0.1 | 50 |
| 20.0/10.0 | 21.0(0.5 | 0.5(0.1 | 9.7(0.3 | 0.90+0.1 | 50 |
| 22.0/11.0 | 22.8(0.8 | 0.5(0.1 | 10.0(1.0 | 0.90+0.1 | 50 |
| 25.0/12.5 | 25.8(0.8 | 0.5(0.1 | 11.0(1.0 | 0.90+0.1 | 25 |
| 28.0/14.0 | 28.8(0.8 | 0.5(0.1 | 13.0(1.0 | 0.90+0.1 | 25 |
| 30.0/15.0 | 30.8(0.8 | 0.5(0.1 | 14.0(1.0 | 1.00+0.2 | 25 |
| 35.0/17.5 | 35.8(0.8 | 0.5(0.1 | 16.0(1.0 | 1.00+0.2 | 25 |
| 40.0/20.0 | 42.0(1.5 | 0.5(0.1 | 19.0(1.0 | 1.00+0.2 | 25 |
| 50.0/25.0 | 51.0(1.0 | 0.5(0.1 | 24.0(1.0 | 1.00+0.2 | 25 |
| SIZE | I.D.OF AS SUPPLY (mm) | WALL OF AS SUPPLY (mm) | I.D OF AFTER RECOVERED (mm) | WALL OF AFTER RECOVERED (mm) | LENGTH PER COIL (m) |

标准颜色：黑、白、红、黄、兰、绿、灰

STANDARD COLOR：BLACK、WHITE、RED、YELLOW、BLUE、GREEN、GREY