ZRG系列辐射交联

# 低压母线保护套管

# ZRG series-Low Voltage Heat Shrinkable Bus-bar Tubing

- 难燃性：VW-1；

- 耐热性：最高使用温度可以达到125(C；

- 低温性：在-55(C温度环境中，产品不脆不裂；

- 安全性：使用在1KV及以下的配电系统中，可以缩短相间和对地的距离；

- 使用方便：产品具有连续长度，可满足各种长度母线排的需要；

- 标识容易：产品具有多种颜色可供选择；

- ZRG系列产品在1999年通过了江苏省新产品鉴定验收，在2000年被认定为江苏省高新技术产品，产品编号：000500G0030N。

CHARACTERISTICS :

| Property | Test Condition | Performance |
| --- | --- | --- |
| Tensile strength |  | 12Mpa minimum. |
| Elongation |  | 400% minimum. |
| Tensile strength after aging | After 7 Days Air Oven at 158(C | 10Mpa minimum. |
| Elongation after aging |  | 300% minimum |
| DEFORMATION TEST | 1 hr at 131(C | 25% maximum. |
| HEAT SHOCK TEST | 4hr at 250(C | No Cracking |
| FLEXIBILITY TEST | 7 Days Air Oven at 158(C | No Cracking, No Permanent Deformation |
| CONDUCTOR CORROSION | 7 Days Air Oven at 158(C | No Corrosion |
| Volume Resistivity |  | 1014 (.cm minimum. |
| Dielectric withstand |  | No Breakdown for 60 sec.at 2.5KV |
| Breakdown voltage |  | 12KV minimum. |
| Dielectric Strength |  | 25 KV/mm minimum. |
| Dielectric withstand after aging | After 7 Days Air Oven at 158(C | No Breakdown for 60 sec.at 2.5KV |
| Breakdown voltage after aging |  | 12KV minimum |
| COLD BEND TEST | 1hr at -30(C | No Cracking |
| LONGITUDINAL CHANGE | 3 minute Air Oven at 200(C | ( 10% |
| ECCENTRICITY |  | 30% maximum. |
| Flammability |  | VW-1 |
| Minimum Complate Shrink Temperature |  | 100(C（3 minute） |

# ZRG系列主要性能指标:

| 测试项目 | 测试条件 | 测试结果 |
| --- | --- | --- |
| 拉伸强度 |  | ( 12Mpa |
| 断裂伸长率 |  | ( 400% |
| 老化后拉伸强度 | 158(C 烘箱中 放置7天后 | ( 10Mpa |
| 老化后断裂伸长率 |  | ( 300% |
| 热变形试验 | 131(C ，1小时 | ( 25% |
| 热冲击试验 | 250(C，4小时 | 不破裂 |
| 弹性试验 | 158(C，烘箱中7天 | 不破裂、无永久形变 |
| 铜腐蚀试验 | 158(C，烘箱中7天 | 无腐蚀 |
| 体积电阻系数 |  | ( 1014 (.cm |
| 绝缘试验 |  | 2.5KV 60秒 不击穿 |
| 工频耐压强度 |  | ( 12 KV |
| 击穿强度 |  | ( 25KV/mm |
| 老化后绝缘试验 | 158(C 烘箱中 放置7天后 | 2.5KV 60秒 不击穿 |
| 老化后工频耐压强度 |  | ( 12 KV |
| 低温弯曲试验 | -30(C，1小时后 | 不破裂 |
| 纵向收缩比 | 200(C烘箱收缩3分钟 | ( 10% |
| 偏壁率 |  | ( 30% |
| 阻燃性能 |  | VW-1 |
| 完全收缩温度 |  | 100(C（3 分钟） |

# ZRG系列热缩型低压母线保护套管规格表 STANDARD SIZE：

| 规格 SIZE | 收缩后内径 mm I.D. OF AFTER RECOVERED | 收缩后壁厚 mm WALL OF AFTER RECOVERED | 收缩前内径 mm I.D. OF AS SUPPLY | 包装长度 m LENGTH PER COIL |
| --- | --- | --- | --- | --- |
| 60.0/30.0 | < 30.0 | 1.00+0.2 | >60.0 | 25 |
| 70.0/35.0 | < 35.0 | 1.10+0.2 | >70.0 | 25 |
| 80.0/40.0 | < 40.0 | 1.10+0.2 | >80.0 | 25 |
| 90.0/45.0 | < 45.0 | 1.20+0.2 | >90.0 | 25 |
| 100.0/50.0 | < 50.0 | 1.20+0.2 | >100.0 | 25 |
| 120.0/60.0 | < 60.0 | 1.20+0.2 | >120.0 | 25 |
| 150.0/75.0 | < 75.0 | 1.20+0.2 | >150.0 | 25 |
| 200.0/60.0 | < 60.0 | 1.20+0.2 | >200.0 | * |
| 标准颜色：黑、红、黄、绿、兰、白。 STANDARD COLOR：BLACK、RED、YELLOW、GREEN、BLUE, WHITE. 小于60.0mm 的规格请选用DRS系列。The sizes of less than 60.0 mm are same as DRS. * 每根长度1.0米。 The length is 1.0 meter per piece. |